SC-UV-I、 SC-UV-I+型紫外臭氧清洗机

# 名称：紫外臭氧清洗机；                        品牌：北京赛德凯斯；

厂家：北京赛德凯斯电子有限责任公司；      公司网址：www.setcas.com

# SC-UV-I、及SC-UV-I+型紫外臭氧清洗机技术参数如下：

# 紫外臭氧清洗机

# （SC-UV-I不带加热控温功能、SC-UV-I+型集成加热控温功能）

| SC-UV-I型紫外臭氧清洗机(可选配带加热功能：SC-UV-I+型号) |
| --- |
| 产品特色 | 指标 |
| 材质 | 机身整体采用不锈钢材料，耐酸碱、防腐蚀，美观大方 |
| 结构 | 抽屉式样品台，取、放基板简单、方便 |
| 气路 | 预留进气接口，丰富设备的清洗种类 |
| 保护 | 抽屉开合与UV灯工作互锁，避免紫外线伤害 |
| 计时 | 按键定时器，数显倒计时，放便直观 |
| 操作 | 清洗工作进程可以任意时间手动终止 |
| 配件 | 可选臭氧中和器，避免臭氧伤害 |
| 电气 | 指标 |
| 清洗波段 | 185nm和254nm |
| 距离UV灯3-5mm平均光强 | 28~32mW/cm² |
| 灯管 | 双波低压汞灯 |
| 灯管功率 | 150W |
| 照射区域 | 150mm×200mm |
| 可调照射距离 | 5~40mm |
| 定时器工作范围 | 0~99min99s 具有自动倒计时功能 |
| 可选控温范围（仅限SC-UV-I+型号） | 室温–200℃（只适用于SC-UV-I+型号） |
| 机械 | 指标 |
| 进、出气口 | 进气口：φ8mm，出气口：φ25mm |
| 设备外型尺寸 | 250mm（W）×300mm（D）×260mm（H） |
| 托盘外型尺寸 | 160mm（W）×200mm（D）×5~30mm（H） |
| 产品重量 | 8 KG |
| 组成 | UV灯管，工作台，控制面板，系统软件，加热控制模块 |

# UV-Ozone Cleaner

# （SC-UV-I without heating control function、SC-UV-I+ with heating control function）

| SC-UV-I Ozone Cleaner (optional with heating function：SC-UV-I+) |
| --- |
| Feature of product | Index |
| Material | Made of stainless steel，which is resistant to acid and alkali, anti-corrosion |
| Structure | Drawer type sample stage, easier to take and place substrate |
| Air channel | Reserved intake port, a wide variety of cleaning equipment |
| Protection | The drawer opening and closing are interlocked with the UV lamp to avoid UV damege |
| Timer | Button timer, digital countdown, easy to look at it |
| Operation | The cleaning process can be manually terminated at any time |
| Accessories | Optional ozone neutralizer to avoid ozone damage |
| Electric | Index |
| Cleaning wave band | 185nm和254nm |
| Average light intensity at a distance of 3-5mm from the UV lamp | 28~32mW/cm² |
| Light tube | Dual wave low pressure mercury tube |
| Light tube power | 150W |
| Irradiation area | 150mm×200mm |
| Adjustable irradiation distance | 5~40mm |
| Timer range | 0~99min99s with automatic countdown function |
| Heating area (SC-UV-I+model only) | Room temperature –200℃ (suitable for SC-UV-I+model) |
| Mechanical | Index |
| Air intake,Air outlet | Air intake：φ8mm，Air outlet：φ25mm |
| Outer dimension of the device | 250mm（W）×300mm（D）×260mm（H） |
| Tray outer dimension | 160mm（W）×200mm（D）×5~30mm（H） |
| Product Weight | 8 KG |